## Slide 1: METAL CASTING

## Slide 2: Metal Casting:
It is the process of producing metallic parts by pouring a molten metal in to the mould and allowing the metal to solidify.

## Slide 3: Casting Process
Mould prepared.
Metal is Heated Above Melting Temp.
Liquid Metal Poured into Mold
Metal Solidifies into Shape of Mold
Part Removed from Mold
Post Casting Operations
  Clean Up
  Machining

## Slide 11: Molding sand classification
They can be classified as:
  Natural molding sand (Green sand)
- Taken from river beds & contain major amount of clay
- easily available at low cost
  Synthetic sand
  - contain little or no binder (clay)
  - strength & bonding property can be easily controlled
  - more expensive than natural sand
  Special sand
    - ideal in getting special characteristics..

## Slide 12: Sand preparation
Very few natural sands have all the qualities required by a molding sand
It is mixed with other sands which possess the required characteristics
Sufficient moisture must be added to the sand
Sand must be properly conditioned before use

## Slide 13: Properties of a molding sand
Porosity (permeability)
  Sand must be porous to allow the gases/ moisture present within the molds to be removed freely when molten metal is poured
Adhesiveness
  sand particles must be capable of adhering to sides of molding boxes
Cohesiveness / Strength
  Ability of sand particles to stick together
  Should be sufficient to permit the mold to be formed to the desired shape even after the hot metal is poured in the mold
Refractoriness
  Molding sands with a poor refractoriness may burn on to the casting
  Measured by sinter point of sand

## Slide 14: Properties of a molding sand
Collapsibility
  Mold made out of sand to collapse as the molten metal gets
  solidified in it
Flowability
  Ability of the sand to behave like a fluid so that, when rammed sand will flow to all portions of a mold and around the pattern and take up the required shape
  It increases as clay & water content increase
  High flowability is required of a molding sand of uniform density
  To obtain good impression of the pattern in the mold.

## Slide 15: Gating System

## Slide 16: Components of Gating System
Pouring Basin
Sprue
Sprue base
Runner
In-gate
Riser

## Slide 22: PATTERN
A pattern is an replica of a casting to be made.
Using pattern, impressions (mould cavity) can be formed in the damp sand to make a mould.
Pattern materials
Any material which will retain exact outline of the design for required number of molds

## Slide 23
Wood – easy to work & readily available
– can be cut in to required shapes
– used when small number of castings
Metal - do not change their shape when subjected to moist condition
– used when small number of castings
Plastics – do not absorb moisture, smooth
– can be withdrawn from the mold easily, without damaging the mold
Plaster – High compressive strength
Pattern materials

## Slide 24: Green sand mold

## Slide 25: Basic steps in making sand casting
Pattern making
Core making
Moulding
Melting and pouring
Cleaning

## Slide 26
Green sand mold
with pattern
SECOND OPERATION
Drag
Pattern
Molding board
FIRST OPERATION
Drag
Molding board
Drag
Pattern
Molding board
FIRST OPERATION
Drag
Molding board
Riser pin
Sprue pin
Cope
Parting
line
COMPLETE MOLD
Pouring basin
Weight
Riser
Lifter
Vents
Parting
line
Core
Runner
Gate

## Slide 27
Scooping
It is the process of making a cavity in the sand mould
without using a pattern.
Instead it makes use of casting hand tools like shovel,
rammer etc.

## Slide 28
Types of patterns
Single piece pattern
Match plate pattern
Gated pattern
Split pattern
Cope & Drag pattern
Loose-piece pattern
Skeleton pattern

## Slide 30
Made from one piece & does not contain loose pieces
Inexpensive & are of simplest type
Single piece pattern
Split pattern
Most widely used pattern for intricate castings
Here the pattern is split in to 2 parts so that one part is in
the cope & other is in the drag
Two halves of the pattern is aligned properly by using
dowel pins

## Slide 31
Similar to split patterns
The cope & drag halves of the pattern along with the gating
and risering systems prepared separately
But they are attached separately to the metal or wooden
plate along with alignment pins
Cope and Drag pattern
Match plate pattern
An extension of cope and drag pattern
Here the cope & drag patterns along with the gating &
risering are mounted on a single matching or metal plate
on either side

## Slide 32
Used when contour of the part is such that withdrawing the
pattern from the mold is not possible
Obstructing part is held as a loose piece
Loose piece pattern
Skeleton pattern
Made of strips of wood for preparing final pattern
by pouring the sand around the pattern and packing it

## Slide 33
Usually made of metal which increases their strength and
reduces tendency to warp
Section connecting different patterns serve as runner
and gates
A gated pattern can manufacture many castings at one
time
Used in mass production systems
Gated pattern

## Slide 34
Pattern Allowances
Shrinkage allowance
Machining or Finishing allowance
Draft or Taper allowance
Camber or distortion allowance
Shake or Rapping allowance
Mould wall movement allowance

## Slide 35
Pattern Allowances
Shrinkage allowance
Most of the metals used in casting contract during cooling from pouring temperature to room temperature
Provided to compensate for solid contraction by providing adequate allowances in the pattern
Amount of contraction varies with different metals

## Slide 37
Pattern Allowances
2. Machining allowance
Given on the surface of the pattern by increasing the metal
thickness there to compensate for loss of metal due to
machining on these surfaces
Depends mainly upon method of machining to be employed
Given in addition to the shrinkage allowance

## Slide 38
Pattern Allowances
Given slight taper on the vertical surfaces of the pattern
parallel to the direction of withdrawal from the mould
Provided on both internal & external surfaces
For easy withdrawal of pattern from the mould
3. Draft or Taper allowance

## Slide 39
Pattern Allowances
Negative allowance to be provided in the pattern
When pattern is withdrawn from the mould by striking over
it from side to side, size of the cavity increases
To compensate this rapping allowance is provided
4. Rapping allowance

## Slide 40
Pattern Allowances
Castings having irregular shape, will not have uniform
contraction during their cooling
Results in distortion of the castings
Remedy:
An opposite distortion is provided in the pattern
5. Distortion allowance

## Slide 42
Pattern Allowances
Mould wall movement takes place because of excessive
heat and pressure applied by the molten metal on the surface
layer of the sand
Affects the size of the casting
Remedy:
  Provide proper allowance in the pattern
  Controlling the density & temperature of molten metal
  Controlling the composition of the molding sand
6. Mould wall movement allowance

## Slide 43: DEFECTS IN METAL CASTING

## Slide 44: CLASSIFICATION OF CASTING DEFECTS
Gas Porosity Defects
  Pinholes
  Subsurface Blowhole
  Open hole
  2. Shrinkage Casting Defects
  Open Shrinkage defects
  Closed Shrinkage defects
  3. Mould Material casting defects
  Cuts and Washes
  Fusion
  Runout
  Swells
  Drops
  Rat tails, veins and buckles
  Metal penetration

## Slide 45
4. Metallurgical Casting Defects
Hot Tear/Crack
Hot/Hard Spots
5. Pouring Casting Defects
Cold Shut/Lap
Misruns
Cold shots
Slag Inclusion (Scab)
6. Casting Shape Defects
Shift/Mismatch
Flash, Fin & Burrs
Warping

## Slide 46: GAS POROSITY DEFECTS
Pinholes
Pinholes, also sometimes referred to as porosities, are very tiny holes (about 2 mm) usually found in the cope (upper) part of the mold, in poorly vented pockets.
They are always visible to the naked eye and don’t require equipment to identify.

## Slide 47
b) Subsurface Blowhole
Blowholes, or simply blows, are larger cavities than pinholes.
A subsurface blowhole appears on the inside of a cast and usually isn’t visible until after machining.
Subsurface blowholes can be difficult to detect before machining, requiring harmonic, ultrasonic, magnetic or x-ray analysis.
c) Open Holes
These blowholes appear on the surface of the cast and are easier to detect than subsurface blowholes.
Causes and prevention of gas porosity:
There are several causes of cavity defects.
Poor venting of mold and cores.
Insufficient drying of mold and cores.

## Slide 48: SHRINKAGE CASTING DEFECTS
Shrinkage occurs because metals are less dense as a liquid than a solid.
A shrinkage cavity is a depression in a casting which occurs during the solidification process.
Large shrinkage cavities can undermine the integrity of the casting and may cause it to eventually break under stress.
Shrinkage can result in two types of casting defects.

## Slide 49
a) Open Shrinkage defects
These are open to the atmosphere. Air compensated as the shrinkage cavity forms.
Pipes are open shrinkage defects that form at the surface and burrow into the casting.
Caved surfaces are shallow, open shrinkage defects that form across the surface of the casting.

## Slide 50
b) Closed Shrinkage defects
Also known as shrinkage porosity, closed shrinkage defects form within the casting.
Macro shrinkage can be viewed with the naked eye, but micro shrinkage cannot.
Closed shrinkage defects usually appear at the top of hot spots, or isolated pools of hot liquid.

## Slide 51: MOULD MATERIAL CASTING DEFECTS
Mold material casting defects are related to the mold material, which is most commonly sand.
Cuts and Washes
Cuts and washes are areas of excess metal.
These appear when the molten metal erodes the molding sand.
A cut appears as a low projection along the surface of the drag face, decreasing in height as it extends from one side of the casting to the other.

## Slide 52
b) Fusion:
Fusion occurs when sand grains fuse
with molten metal.
It appears as a thin crust with a brittle,
glassy appearance firmly adhered to the casting.
c) Run out:
Run out is when liquid metal leaks out
of the mold, leading to an incomplete
or missing casting.
d) Swells:
Swells are an enlargement of the casting.
Swells typically take on the shape of a slight,
smooth bulge on the vertical face of castings.

## Slide 53
e) Drops
Drops occur when pieces of sand fall into metal
casting when it’s still liquid.
Drops appear as an irregularly shaped
projection on the cope (top) surface of a casting.
f) Rat tails, veins and buckles
Rat tails, or veins, appear as an irregular
line or crack on the casting, when the surface
of the molding sand buckles up.
Rat tails usually occur on the surface of the
mold bottom, an area covered with molten
material.
Buckles are a more severe form of rat tails.

## Slide 54
g) Metal Penetration
Metal penetration occurs when liquid metal penetrates gaps in the molding sand.
The penetration is visible to the naked eye as a rough and uneven surface finish of the casting.

## Slide 55: METALLURGICAL CASTING DEFECTS
Hot Tear/Crack
Cracks appear in the form of irregular
crevices in a branched pattern.
Cracks occur as the casting cools,
towards the end of solidification.
b) Hot/Hard Spots
Hot spots are spots that are harder than the surrounding area.
This is because they cooled more quickly than the surrounding material.
Hard spots can interfere with machining and increase tool wear.

## Slide 56: POURING CASTING DEFECTS
Cold Shut/Lap:
Cold shut is a type of surface defect. You will see a line or crack with a round edge on the casting surface.
This defect is visible to the naked eye and often results in rejecting the cast, as it creates a weak spot.

## Slide 57
b) Misruns:
Misruns occur when the liquid metal is
too cold to flow to the extremities of the
mold cavity before freezing and solidifying.
The liquid metal does not completely
fill the mold cavity.
The misrun is the unfilled portion or space in the mold.
c) Cold Shots:
Splattering during pouring of a liquid
can cause solid globules to form.
As these globules freeze, they become
entrapped in the casting.
Cold shots are typically ball, drop or
pearl shaped and loosely attached to the metal.

## Slide 58
d) Slag Inclusion (Scab)
These irregular metallic crusts are found on the casting surface.
Scabs are typically only a few millimeters thick but can be seen by the naked eye.
Scabs are closely related to rat tails and they usually appear together.
Removal of scabs will typically reveal a rat tail underneath.

## Slide 59: CASTING SHAPE DEFECTS
Shift/Mismatch:
Mold shift is due to misalignment of upper (cope) and lower (drag) part of the mold.
Mold shift is usually reflected as a horizontal displacement.

## Slide 60
b) Flash, Fin & Burrs
Flash is one of the most frequently occurring casting defects and also a common injection molding defect.
Flash, also known as casting fin or burrs, is any unwanted and excess material attached to a cast.
It’s typically a thin sheet of metal that forms at the parting faces.
Flash is a waste material that turns into dross after being re-melted.

## Slide 61
c) Warping:
Warping is an unwanted casting deformity that can occur over time, which results in a change in the dimensions of the final product.
It can happen during or after solidification.